BL3 Compaund

| Density | 0.950-0.960 q/cm3 |
| --- | --- |
| MFR (190°C/5 kg) | 1.2±0.3 q/10min |
| Color | sarı |
| Ash content | <1% |
| OIT (200-210 °C) | ≥20 |
| Free from humidity and non-polymer substances such as |  |
| stone, iron, rubber particles, etc |  |

Dırector of Grand Supplier_________	Signature_________