GPI7548

| Propertıes | Standard and Test Method | Unıt | Typıcal Value |
| --- | --- | --- | --- |
| Hardness | ASTM D2240(15sec) | Shore A | 81±2 |
| Density | ASTM D792 / IEC 60811-1-3 | gr/cm³ | 1.48±0.02 |
| Heat Stability at 200°c | VDE 0472/9.71 | minute | min 80 |
| Properties before ageing |  |  |  |
| Tensile strength | IEC 60811-1-1 | N/mm² | min 13 |
| Elongation at break |  | % | min 250 |
| Properties after ageing “7 days at |  |  |  |
| 100°c” | IEC 60811-1-2 | % | max 25 |
| Variation of Tensile |  | % | max 25 |
| Variation of Elongation |  |  |  |

Director of Grand Supplier______	 Signature____