HFFR CABLE COMPOUND

HFK-138

| No. | Name of the indicator | Min. meaning | Max. meaning | Fact. meaning |
| --- | --- | --- | --- | --- |
| p/p |  |  |  |  |
| 1 | Tensile strength, MPa | 10 |  | 11.9 |
| 2 | Relative elongation at break, % | 150 |  | 179 |
| 3 | MFR (150; 21.6), g/10 min | 5 |  | 7.5 |
| 4 | Density, g/cm3 |  | 1.55 | 1.50 |
| 5 | Hardness, Shore D | 45 | 55 | 47 |
| 6 | The amount of foreign inclusions up to |  | 30 | 10 |
|  | 0.5 mm |  |  |  |
| 7 | The appearance of the harness must |  |  | Corresponds |
|  | match the control sample. |  |  |  |
|  | Surface of the cut of the tourniquet |  |  |  |
| 8 | (pores visible to the naked eye are not |  |  | Corresponds |
|  | allowed) |  |  |  |

Director of Grand Supplier_________                                                               Signature________