HFFR CABLE COMPOUND

HFK-238

| No. | Name of the indicator | Min. meaning | Max. meaning | Fact. meaning |
| --- | --- | --- | --- | --- |
| p/p |  |  |  |  |
| 1 | Tensile strength, MPa | 10 |  | 12.9 |
| 2 | Relative elongation at break, % | 150 |  | 185 |
| 3 | MFR (150; 21.6), g/10 min | 5 |  | 12.3 |
| 4 | Density, g/cm3 |  | 1.55 | 1.49 |
| 5 | Hardness, Shore D | 45 | 55 | 47 |
| 6 | The appearance of the harness must |  |  | Corresponds |
|  | match the control sample. |  |  |  |
|  | Surface of the cut of the tourniquet |  |  |  |
| 7 | (pores visible to the naked eye are not |  |  | Corresponds |
|  | allowed) |  |  |  |

Director of Grand Supplier___________                                                          Signature__________