Thermoplastics (TEP, TRE, TRE-S)

MASFLEX 45D110NAT9100

|  | Features | Measurement method |  | Unit of measurement |  | Indicators |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Physical |  |  |  |  |  |  |
|  | Density | GOST 15139 |  | g/cm3 |  | 1,01±0,01 |  |
|  | Shore D hardness | GOST 263-75 |  | conl. units |  | 45±1 |  |
|  | Conditional tensile strength, not less than | GOST 270-75 |  | MPa |  | 15 |  |
|  | Elongation at break, not less than | GOST 270-75 |  | % |  | 550 |  |
|  | PTR (190°C, 5 kg) | GOST 11645-73 |  | g/10min. |  | 30±15 |  |
|  | Electrical strength, not less than | GOST 6433.3 |  | kVsQ/mm |  | 16 |  |
|  | Specific surface resistance, not less than | GOST 6433.2 |  | Om |  | 4*10^15 |  |
|  | Specific volume resistance, not less than | GOST 6433.2 |  | Om*m |  | 2*10^13 |  |
|  | UV resistance (370nm) | - |  | - |  | - |  |
|  |  |  |  |  |  | persistent |  |
|  | Water absorption, |  |  |  |  |  |  |
|  | no more than | GOST 4650 |  | % |  | 0,2 |  |
|  | Thermal |  |  |  |  |  |  |
|  | Temperature limit of brittleness, not higher | GOST 7912-74 |  | °C |  | - 50 |  |
|  |  | Recommended processing modes |  |  |  |  |  |
|  | Temperature of the 1st zone | - |  | °C |  | 175±10 |  |
|  | Temperature of the 2nd zone | - |  | °C |  | 180±10 |  |
|  | Temperature of the 3rd zone | - |  | °C |  | 190±10 |  |
|  | Melt temperature | - |  | °C |  | 190±10 |  |
|  | Mold/Die temperature | - |  | °C |  | +35 |  |
|  | Casting pressure | - |  | - |  | average |  |
|  | Injection rate | - |  | - |  | medlum-fast |  |
|  | Drying | - |  | - |  | basically not required |  |
|  | Maximum safe processing temperature. | - |  | °C |  | 250 |  |

Director of Grand Supplier______	Signature_____