Thermoplastics (TEP, TRE, TRE-S)

MASFLEX 45D112BLK9010U

| Features | Measurement method | Unit of measurement | Indicators |
| --- | --- | --- | --- |
| Physical |  |  |  |
| Density | GOST 15139 | g/cm3 | 1,18±0,01 |
| Shore D hardness | GOST 263-75 | conl. units | 47±2 |
| Conditional tensile strength, not less than | GOST 270-75 | MPa | 15 |
| Elongation at break, not less than | GOST 270-75 | % | 550 |
| PTR (190°C, 5 kg) | GOST 11645-73 | g/10min. | 3±2 |
| Electrical strength, not less than | GOST 6433.3 | kVsQ/mm | 16 |
| Specific surface resistance, not less than | GOST 6433.2 | Om | 4*10^15 |
| Specific volume resistance, not less than | GOST 6433.2 | Om*m | 2*10^13 |
| UV resistance (370nm) | - | - | persistent |
| Water absorption, |  |  |  |
| no more than | GOST 4650 | °C | 0,2 |
| Thermal |  |  |  |
| Temperature limit of brittleness, not higher | GOST 7912-74 | °C | - 50 |
|  | Recommended processing modes |  |  |
| Temperature of the 1st zone | - | °C | 175±10 |
| Temperature of the 2nd zone | - | °C | 180±10 |
| Temperature of the 3rd zone | - | °C | 190±10 |
| Melt temperature | - | °C | 190±10 |
| Mold/Die temperature | - | °C | 190±10 |
| Casting pressure | - | - | - |
| Injection rate | - | - | - |
| Drying | - | - | basically not required |
| Maximum safe processing temperature. | - | °C | 250 |

Director of Grand Supplier______	Signature_____