P P - X L P 1 2 B C Silane

Cross-linkable Polyethylene

Compound

| Properties | Standard and Test Method | Unit | Typical Value |
| --- | --- | --- | --- |
| Melt Flow Index (190°c/5kg) | ASTM D1238 | gr/10min | 4±0.5 |
| Hardness | ASTM D 2240 (15sec) | Shore D” | 50±2 |
| Density | ASTM D 792 / IEC 60811-1-3 | gr/cm³ | 0.945±0.01 |
| Properties before ageing |  |  |  |
| Tensile strength | IEC 60811-1-1 | N/mm² | min 14.5 |
| Elongation at break |  | % | min 200 |
| Properties after ageing “10 days at 150°c” |  |  |  |
| Variation of Tensile | IEC 60811-1-2 | % | max 25 |
| Variation of Elongation |  | % | max 25 |
| Hot Set Test (200°C,0.3MPa) |  |  |  |
| Elongation under load | IEC 60811-2-1 | % | max 100 |
| Permanent elongation after cooling |  | % | max 15 |
| Carbon black content | ASTM D1603 | % | 2.5±0.5 |

| Director of Grand Supplier_________ | Singature_________ |  |
| --- | --- | --- |