PP- XLP13 Silane Cross-linkable

Polyethylene Compound

| Properties | Standard and Test Method | Unit | Typical Value |
| --- | --- | --- | --- |
| Melt Flow Index (190°c/5kg) | ASTM D1238 | gr/10min | 3±0.5 |
| Hardness | ASTM D 2240 (15sec) | Shore D” | 54±2 |
| Density | ASTM D 792 / IEC 60811-1-3 | gr/cm³ | 0.92±0.005 |
| Properties before ageing |  |  |  |
| Tensile strength | IEC 60811-1-1 | N/mm² | min 15 |
| Elongation at break |  | % | min 400 |
| Properties after ageing “7 days at 135°c” |  |  |  |
| Variation of Tensile | IEC 60811-1-2 | % | max 25 |
| Variation of Elongation |  | % | max 25 |
| Hot Set Test (200°C,0.2MPa) |  |  |  |
| Elongation under load | IEC 60811-2-1 | % | max 100 |
| Permanent elongation after cooling |  | % | max 10 |

Director of Grand Supplier___________                                                                          Signature__________