PP-M94

| Phısıcal | Standart and Method | Unıt | Value |
| --- | --- | --- | --- |
| Density | IEC60811-606 | g/cm3 | 0.945 |
| Melt Flow Index(190C/2.16kg) | IEC60811-511 | g/10min | 0.75 |
| Melt flow index(190C/5Kg) | IEC60811-511 | g/10min | 3 |
| Carbon black conten | ASTM D 1603 | % | 2.4 |
| Carbon black Dispertion | ISO18553 | - | 2.5 |
| Tensile strength | IEC60811-501 | N/mm2 | 32 |
| Elongation at break | IEC60811-501 | % | 840 |
| E.S.C.R | ASTM D1693 | Hour | >1000 |
| Hardness | ASTM D2240 | ShoreD | 58 |
| Volume resistivity | IEC60093 | cmὨ | 1015 |
| Dielectric strength(2mm thickness) | IEC60243 | KV/mm 2 | Nobreakdowm at 10 |

| Director of Grand Supplier________ | Signature___________ |  |
| --- | --- | --- |